| Single-layered Materials (fabric) with Thin Nanostructured Films |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Material grade | Frequency range from 3 to 40 GHz |  |  |  | Thickness mm | Specific weight kg/m2 |
|  | Dielectric constant |  | Magnetic permeability |  |  |  |
|  | Real | Imaginary | Real | Imaginary |  |  |
| 1PP8M2-1 | 100-1000 | 100-200 | 1.5-4.0 | 1-5 | 0.8 - 2.0 | 0.08 – 0.15 |
| 1PPM8M10-1 | 1000-5000 | 100-500 | 1.5-4.0 | 1-5 |  |  |
| Microwave & InfraRed Multi-layered Materials (fabric) with Thin Nanostructured Films |  |  |  |  |  |  |
| Material grade | Wavelength ranges |  | Reflectivity dB |  | Thickness mm | Specific weight kg/m2 |
| 1PP8M10-6 | 15 cm to 1 mm |  | -10…-30 |  | 1-4 | 1-1.5 |
|  | 1 mm to 760 nm |  | -20…-30 |  |  |  |
|  | 760 nm to 400 nm |  | -20…-30 |  |  |  |
| 1PP8M10-8 | 30 cm to 1 mm |  | -8…-30 |  | <3 | 1-1.5 |
|  | 1 mm to 760 nm |  | -20…-30 |  |  |  |
|  | 760 nm to 400 nm |  | -20…-30 |  |  |  |
| Operational temperatures from -60 to +85 °C. Maximum dimensions of the Single- and Multi-layered Materials are 600x600 mm. Manufacturing of the materials with customized dimensions and shapes is possible. |  |  |  |  |  |  |