|  |  |
| --- | --- |
| Amount of preparation, mm | up to 90x90 |
| Working area, mm | up to 85x85 |
| Number of strokes per mm | 70 – 600 |
| Operating spectral range | visible and near IR |
| Relative efficiency for the working wavelength,% | >40 |
| Resolution in the first working order | 0.9 |