|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Substrate material | Working spectral rangeum | The maximum value of the transmittance, not less than,% | Relative half-width,% | The average value of the transmission coefficient in the blocking area, not more than,% |
| Glass | 0,4…1,1 | 20 | 1,5…5,0 | 0,2 |
| Silicon, germanium | 3…5 | 30 | 1,0…2,0 | 0,1 |
| Germanium | 8…12 | 30 | 1,0…2,0 | 0,1 |