| Flat grilles | Вогнутые решетки |
| --- | --- |
| Amount of preparation, mm | up to 320 x 220 x 40 | 25 – 120 |
| Working area, mm | up to 300 x 200 | 20 – 120 |
| Number of strokes per mm | 300 – 3600 | 300 – 3600 |
| Operating spectral range, nm | 50 – 2500 | 100 – 1500 |
| Relative diffraction efficiency for the working wavelength,% | up to 70% | 40 – 60 |
| Resolution in the first working order (from theoretical value) | 0.9 | 0.9 |