Физико-химические характеристики:

| Внешний вид | Порошок белого цвета |
| --- | --- |
| Потери массы при прокаливании, % | 6-14 |
| Массовая доля соединений цинка, %: - в пересчете на Zn; - в пересчете на ZnO; | 40-50 49-60 |
| Массовая доля соединений фосфора, %, не менее: - в пересчете на РО4; - в пересчете на P2O5; | 40 30 |
| Массовая доля веществ, растворимых в воде, %, не более | 0,3 |
| Остаток после мокрого просеивания на сите с сеткой 0,045, %, не более | 0,3 |
| рН водной суспензии | 5,5-8,0 |
| Маслоемкость, г/100 г пигмента, не более | 40 |
| Диспергируемость, мкм, не более | 20 |
| Светлота тона, %, не менее | 97 |

TECHNICAL DATA

| Appearance | White powder |
| --- | --- |
| 1. Loss on ignition 600°C (%) | 6-14 |
| 2. Zn content (%) ZnO content (%) | 40-50 49-60 |
| 3. PO4 content (%) P2O5 content (%) | 40 30 |
| 4. Mass fraction of substances soluble in water %, max | 0,3 |
| 5. Sieve residue - 45 μm (%), max | 0,3 |
| 6. рН water suspension | 5,5-8,0 |
| 7. Oil absorption (cm3 /100g), max | 30 |
| 8. Dispersibility mkm, max | 20 |
| 9. Tone light , %, min | 98 |

Formulators Guidelines

| Solvent Borne | Performance |  |
| --- | --- | --- |
| Short Oil Alkyd |  |  |
| Medium oil Alkyd |  |  |
| Long oil Alkyd |  |  |
| 2K Epoxy |  |  |
| High Solid Epoxies |  |  |
| Epoxy Ester |  |  |
| PU |  |  |

| Water Borne | Performance |  |
| --- | --- | --- |
| Water reducible Alkyd |  |  |
| Alkyd emulsion |  |  |
| Epoxy Ester |  |  |
| 2K Epoxy |  |  |
| Acrylics and Modified acrylics |  |  |

| Powder | Performance |  |
| --- | --- | --- |
| Polyester |  |  |
| Silicone |  |  |
| Epoxy |  |  |

| Speciality coatings | Performance |  |
| --- | --- | --- |
| Wash primers |  |  |
| Coil Coatings |  |  |